Tender Specifications AVK Surface Box MPVH LD-GG [80/22-722]

1. Range

Surface Box MPVH / height adjustable 230-300 mm / PA+

2. Product description

General

The surface box shall be for installation in tarmac roads to provide access to underground valves in water or gas lines.

Basic design

The surface box design shall correspond with AVK Surface Box MPVH LD-GG series 80 type 22 variant 722 (STV 80/22-722) or equivalent.

Product shall be a heat resistant, synthetic surface box with a cast iron GJL-200 lid attached to the housing by a galvanized steel cable.

Housing shall consist of two parts made out of heat resistant PA+ material with a fixed bottom part and a floating type height adjustable top part.

Upper rim of top part shall be hexagonal.

Features

Surface box shall have a max. total weight of 2 Kg.

Housing shall be 100% corrosion-free.

Housing and lid shall be designed to ensure easy opening at all times

Surface box housing and lid shall have a heat resistance of at least 250 °C.

Surface box shall be equipped with click system to ensure lid will stay in place

Surface box shall meet D400 load bearing capacity, tested by applying flat load on top surface.

Surface box shall have a height range of 230-300 mm.

Top part shall be able to be turned 360 degrees during installation for easy positioning of lid inscription.

Floating top part shall follow road settlement ensuring perfect alignment at all times.

3. Sustainability

Surface box shall have a carbon footprint of max. 3 Kg. Carbon footprint (CO2 emission) shall be calculated by using Lifecycle Assessment method according to ISO 14040-44. 
Housing to be made of 100% first grind recycled thermoplastic material.

Housing and lid to be 100% recyclable after end of life.

Surface box shall contain no heavy metals or any other contamination.